Firing cheat sheet

Bisque

Loading

- Arrange pots according to size

- Check for dust in kiln

- As you load shelves, dust top and scrape bottoms

- Check that cable is elevated off the floor

- Clean top and bottom of posts before inserting into kiln (kiln wash on post can make them stick to shelves)

- Witness cone pack inserted in kiln near peep holes

- Remember: mugs should be loaded with handles facing inward

Programming the computer controlled kilns

- Turn power on

- Should see IDLE if not, press ENTER

- Press slow bisque

- ENTER

- Type cone #. Example: Bisque:  06 (optional cone 05 to burn off additional impurities in clay)

- ENTER

- IDLE TC 2 will display briefly, then current temperature

- Setting preheat to extend the firing schedule (Remember must be present for first and last 2 hours of firing)

  - Press other x2 to set preheat (Slow bisque cone 06 ~ 12 hrs)

  - Preheat time = # of hours until you want firing to end – 12 (firing time) - 1 to bring temperature to preheat

  - Example below: kiln start at 8 pm which is 15 hours away from 11 am: 15-12-1 = 2 hours preheat required

  - For  2 hours, type 200 then ENTER

- Review program

- Press START

- Last minute check:

  - Peep holes closed

  - Latch is on

  - Fans are on

  - Make sure lid is aligned with bottom (Kiln 2 & 3 in particular)

Firing is completed:

- Register ending temperature & length of time

- Turn off kiln

- Close fans

- Crack the lid and open the peeps when the temperature is about 100° C or 200° F

- Kiln lid may be open when the temperature is down to 52° C (125° F) or below.

Unloading

- Inspect and record shelves in book, scrape and kiln wash those requiring attention

- Vacuum kiln thoroughly

GLAZE

Loading

- Arrange pots according to size

- Check for dust in kiln

- As you load shelves, dust top & scrape bottoms

- Cables elevated off the floor

- Clean top and bottom of posts before inserting into kiln (kiln wash on post can make them stick to shelves)

- Ensure bottoms of pots are cleaned, use cookies when possible.

- Witness cone pack inserted in kiln near peep holes

Programming the computer controlled kilns

- Turn power on

- You should see IDLE, if not press ENTER

- Press slow glaze

- ENTER

- Enter cone

  - Glaze 6 (optional cone 5 with 15 minute hold)

to correct press 000 then enter

- ENTER

- Soak or hold (10-30 minutes) or leave at 0

- ENTER

- IDLE TC 2 will display briefly, then current temperature

- Setting preheat to extend the firing schedule (Remember must be present for first and last 2 hours of firing)

  - Press other x2 to set preheat (Slow glaze cone 6 ~ 9 hrs)

  - Preheat time = # of hours until you want firing to end – 9 (firing time) - 1 to bring temperature to preheat

  - Example below: kiln start at 8 pm which is 13 hours away from 9 am: 13-9-1 = 3 hours preheat required

  - For  3 hours, type 300, then ENTER

- Review program

- Press START

- Last minute check:

  - Peep holes closed

  - Latch is on

  - Fans are on

  - Make sure lid is aligned with bottom (Kiln 2 & 3 in particular)

Firing is completed:

- Register ending temperature & length of time

- Turn off kiln

- Close fans

- Crack the lid and open the peeps when the temperature is about 100° C or 200° F

- Kiln lid may be open when the temperature is down to 52° C (125° F) or below.

Unloading

- Inspect and record shelves in book, scrape and kiln wash those requiring attention

- Vacuum kiln thoroughly